<page>002v</page>

<image>http://gallica.bnf.fr/ark:/12148/btv1b10500001g/f10.image</image>

<div>

<id>p002v\_1</id>

<it/><ab>Practica, cioè nova inventione di contegiare, stampata in <pl>Brescia</pl> per Vincenzo Sabio<comment>c\_002v\_01</comment>.</ab>

</div>

<div>

<id>p002v\_2</id>

<head><add><m>Emeralds of <pl>Brissac</pl></m></add></head>

<ab>I have taken <m>minium</m>, 26 <ms><figure>℥</figure></ms>, <m>crystal</m> <add><ill/> and ground on <tl><m>marble</m></tl></add> 12 <ms><figure>℥</figure></ms>, <m>verdet</m> 3 <ms><figure>|ʒ|</figure></ms>. Incorporate all together, put in a <tl>crucible covered by another well <m>luted</m> that has a hole in the top</tl>. Fusion 7 <ms><tmp>hours</tmp></ms> without blowing. The mass has been of a beautiful green.</ab>

<ab>I have taken <m>minium</m> 12 <ms><figure>℥</figure></ms>, <m>crystal</m> 6 <ms><figure>℥</figure></ms>, <m>verdet</m> 2 <ms>grains</ms>. Fusion soft vi <ms><tmp>hours</tmp></ms>, cooked again 24 <ms><tmp>hours</tmp></ms>. The mass has been of green, yellow, &amp; red.</ab>

</div>

<div>

<id>p002v\_3</id>

<head><m>Sapphire</m></head>

<ab><m>Pebbles</m> or <m>crystal</m> 8 <ms><figure>℥</figure></ms>, <m>minium</m> 16 <ms><figure>℥</figure></ms>, <m><pro>blacksmith</pro>'s salt</m> 4 <ms><figure>℥</figure></ms>, sparkling <unc><m><fr>coryal</fr></m></unc><comment>c\_002v\_02</comment> 4 <ms>grains</ms>. Fusion <unc>6</unc> <ms><tmp>hours</tmp></ms>.</ab>

</div>