<page>048v</page>

<image>http://gallica.bnf.fr/ark:/12148/btv1b10500001g/f102.image</image>

<div>  
<id>p048v\_a1</id>  
<head>Regulus extraction</head>

<ab>Take one lb. of <m>antimony</m>, half a lb. <m>black soap,</m> and half a lb. of <m>tartar</m> from <pl>Montpellier</pl>. Once the whole is pulverized, one needs to boil in a <m>varnished earthenware pot</m> on a big <m>fire</m> while stirring the whole often with a <m>pick of wood or iron</m>, &amp; the said <m>soap</m> will be consumed and burn off and the rest will stay more or less red, and it will be necessary that it is reduced by a third. Then one needs to throw it on a <m>tile</m> and it will turn blackish. One will need to melt this four or five times and pour it on the flat <m>tile</m> and then you will have the regulus drawn from antimony.</ab>

<ab>Others pulverize the <m>antimony</m> &amp; mix it with <m>saltpeter</m> &amp; pulverized <m>tartar</m>, as much of one as of the other, &amp;, having heated a <m>pot</m> or <m>crucible</m> red hot, they put a little of it at a time, &amp; <del><fr>se</fr></del> turn their back for fear of the smoke, and continue thus until everything is put in, and strengthen the <m>fire</m> until everything is thoroughly melted &amp; melt it again several times.</ab>

</div>  
<div>  
<id>p048v\_a2</id>  
<head><m>Lead</m>, <m>tin</m></head>

<ab>They become brittle having been put back to melt, often or for a long time, and they thicken and burn, in such a way that even when one melts a <fr>saulmon</fr>, the <m>tin</m> thickens at the bottom if, while casting, one does not stir it often. It is best for casting to melt a little <m>lead</m> <del>&amp; the</del> or <m>tin</m> &amp; <del><fr>remuer</fr></del> to renew at each melting. The <m>antimony</m> renders them breakable. The <m>looking glass tin</m> whitens them. <del>One</del> <pro>Pewterers</pro> put in <del>on the <m>fine tin</m></del> one <ms>lb</ms> of <m>looking glass tin</m> per one <ms>quintal</ms> of <m>fine tin</m> &amp; two <ms>lb</ms> &amp; a half or three <ms>lb</ms> of <m>red &amp; soft copper of cauldrons</m>, which is better than <m>latten.</m> There is <m>fine &amp; soft tin</m> &amp; <m>brittle tin</m>. The brittle one is cast in <tl><fr>grille</fr></tl> by the <pro>pewterers</pro> to sell it better. <del><fr>O</fr></del> They come out better &amp; more neatly in <tl><m>stone</m> moulds</tl> than in a <tl><m>copper</m> mold</tl>, because <m>copper</m> is fat &amp; sticks unless one heats the <tl>mold</tl> well or one casts large works. Three <ms>quarters</ms> of <m>lead</m> per one <ms>lb</ms> of <m>soft tin</m>, makes a very liquid line &amp; proper for casting, which has a shine like a mirror. <m>Sandever</m> lightens them. All things that lighten well <m>metals</m> &amp; remove their thickness &amp; dense nature &amp; render them <del>like</del> liquid like <m>water</m>, render them proper for casting, for it is the thickness that prevents them from running. <m>Soft tin</m> is more even <del><fr>com</fr></del> than the <m>brittle one</m>, which is whiter and seems to be burnished like a mirror.</ab>

<ab>  
<margin>left-bottom</margin>  
To alloy well <m>tin</m> &amp; <m>lead</m>, one needs to melt one by itself, and then mix in the other, small pieces at a time, and throw it often on the <tl><m>marble</m></tl> or the <tl><m>square tile</m></tl>. And when you will see it become well even <del>like</del> &amp; shiny as if it were burnished, it is good. Because sometimes it becomes spotted due to too much <m>lead</m> &amp; sometimes due to too much <m>tin</m>. There is some <m>tin</m> that has more <m>lead</m> than others. <m>Common tin</m> is the one that is mixed with <m>lead</m>.</ab>

</div>