<page>077v</page>

<image>http://gallica.bnf.fr/ark:/12148/btv1b10500001g/f160.image</image>

<div>

<cont/>

<id>p077r\_4</id>

<ab>but it should not be too small, then take <del><ill/></del> a <tl><m>glass</m> vial</tl> not too big and put into it a half of these two, namely two &amp; a half <ms>ounces</ms>. Next take the said <m>benzoin just as roughly crushed</m>, and put it to use with the aforesaid <m>water</m> and let it rest for the space of one &amp; half <ms><tmp>days</tmp></ms>, &amp; then take the said <m>water</m> &amp; put it into another <tl><m>glass</m> vial</tl> &amp; soak it very well. And on the rest of the said <m>benzoin</m> that remains at the bottom of the said first <tl>vial</tl>, put the rest of the <m>water</m> over this and do as before when you see that the case is going well, and mix the first <m>water</m> with the second. By means of this you will be able to help yourself to this for something more noble.</ab>

</div>

<div>

<id>p077v\_1</id>

<head>Another approved <m>varnish</m></head>

<ab>Take two <ms>ounces</ms> of <m><pa>linseed</pa> oil</m> &amp; two <ms>ounces</ms> of <m><fr>huille petrolle</fr></m> and two <ms>ounces</ms> of <m>mastic</m>, the whitest you can find, and of <m><fr>alung de glace</fr></m>, &amp; grind it, and take a little bit of <m>white copperas</m>, and put all these <m>drugs</m> together into an <tl><m>earthen</m> pot</tl> that should be new, and lay it on hot <m>ashes</m> for a bit, and you will see a beautiful <m>varnish</m>.</ab>

</div>

<div>

<id>p077v\_2</id>

<head>Another <m>varnish</m></head>

<ab>Take <m><fr>huille petrolle</fr></m> &amp; <m><pa>spike lavender</pa> oil</m>, as much of one as the other, &amp; mix it together with <m>copperas</m>, &amp; make them melt over hot <m>ashes</m>, according to the quantity that you want to make. To lay down this <m>varnish</m>, put three coats on the work that you want to varnish.</ab>

</div>

<div>

<id>p077v\_3</id>

<head>Another <m>varnish</m></head>

<ab>Take one <ms>ounce</ms> of <m><pa>spike lavender</pa> oil</m> &amp; of <m>sang <del><fr>de ra</fr><del><fr>i</fr></del><add>y</add>e</del> <add>da Rac</add></m><comment>c\_077v\_03</comment> &amp; make</ab>

<cont/>

</div>