<page>100r</page>

<image>http://gallica.bnf.fr/ark:/12148/btv1b10500001g/f205.image</image>

<div>

<id>p100r\_1</id>

<head>Gold color</head>

<ab>To quickly make a layer of <fr><m>or <del><fr>sur</fr></del> mat</m></fr> on <m>canvas</m> or other <m>oil panel</m>, one makes fatty <m><pa>walnut</pa> oil</m> <env>in the sun</env> or <env>on the fire</env>, as said above, for it thickens by itself in this way, although there is neither <m>lead</m>, nor <m>ceruse</m>. And with this, grind <fr><m>massicot</m></fr>, <m>mine</m>, &amp; other desiccatives, not <fr><m>verdet</m></fr> nor <m>orpiment</m>, for they cause the <m>gold</m> to die. It will be dry soon. However, if the <env><tmp>weather is not clear &amp; dry</tmp></env>, do not shade it, for if the <env><tmp>weather is damp &amp; humid</tmp></env>, it would turn black.</ab>

</div>

<div>

<id>p100r\_2</id>

<head>Portrait-painting from nature</head>

<ab>One needs to carefully <sn>observe</sn> the eyes, the nose, &amp; the beard, for these three things make strong resemblance.</ab>

</div>

<div>

<id>p100r\_3</id>

<head><m>Gemstones</m></head>

<ab>One needs to <tl>pestle</tl> your materials in a <tl>mortar of <m>thick glass</m></tl>,&amp; encased &amp; stuck with <m>mastic</m> into another <tl>mortar of <m>wood</m></tl> in order that it does not break, this can serve for <pro>perfumers</pro>, &amp; <del><fr>la t</fr></del> the <tl>pestle</tl> also of <m>glass</m>.</ab>

</div>

<div>

<id>p100r\_6</id>

<margin>left-middle</margin>

<man><margin>left-middle</margin><tl>Mortar of <m>glass</m></tl> and <tl>slab of <m>glass</m></tl> for grinding.</man>

</div>

<div>

<id>p100r\_4</id>

<head>Vitrified <m>saltpeter</m></head>

<ab>

Being melted with <m>pebbles</m>, it makes the <m>glass</m> very white. But before, one needs to calcine it on a <tl>hot tile or coal shovel</tl>. And that which will remain from the vapor, mix it <ms>as much of the <m>white calcined pebbles</m></ms>. It is true that, in the <tl>little furnace</tl>, it is not clarified well. But for large <m>glass</m>, it makes the <m>glass</m> very clear &amp; white &amp; clean.</ab>

</div>

<div>

<id>p100r\_5</id>

<head>Windows through which the <env>sun</env> will not pass</head>

<ab>Take the aforementioned <m>calcined saltpeter</m> &amp; expose it to a <env>humid air or place</env>, and it will convert itself into a liquid which, if rubbed <add>on both sides</add> of the windows, the <env>sun</env> will not pass through; rather, it will give shade. One needs to put the <m>saltpeter</m> on some clean <del>thing</del> <add>place</add>, &amp; <del>it</del> put <tl>glowing coals</tl> on it, and continue all over until it no longer burns.</ab>

<ab>

<margin>left-bottom</margin>

It also serves for melting &amp; for adding in with <m>alkali salt</m> for cleaning <bp>hands</bp>.</ab>

</div>