<page>117r</page>

<image>http://gallica.bnf.fr/ark:/12148/btv1b10500001g/f239.image</image>

<div>  
<id>p117r\_1</id>  
<head>A means of molding flowers and plants</head>

<ab>One needs to choose them in their full verdure &amp; vivacity, &amp; <del><fr>les mou</fr></del> not pick them, if possible, until the time one will want to mold them, so that they do not wilt. Or if you need to carry them from afar, soak their stems in a <tl>bottle of <m>water</m></tl>, or better still <m>wine</m>. Make, firstly, a <m>wax</m> stick pointed like a big peg, of a size appropriate to what you want to cast, as you see in the margin, marked A. Put &amp; prick at the foot of this small peg a bit of <m>iron wire</m>, rather thick &amp; strong. And at the point of this, you will fit your flower stem or your plant. This done, set it aside neatly. And arrange your <del><tl>mold</tl> of t</del> circle &amp; shape of <m>clay</m> as you have done for the <al>snakes</al>, in the form of a <mu>mandore</mu> <del>in such a way that</del> according to the size of your plant. Then take the one that you have prepared to be cast, as we have taught you, &amp; wet &amp; moisten it very carefully with <m>good <add>eau-de-vie</add></m> with a <tl>pinceau</tl>. Then pass the <tl>wire stem</tl> through the end of the <m>earthen</m> <mu>mandore</mu>, in order that the <m>wax</m> <del><fr>q</fr></del> peg, where the plant is fastened, joins to the end of the <m>earthen</m> <mu>mandore</mu>. And arrange thusly your plant in such a way lying down that it remains in the middle of aforesaid <mu>mandore</mu>, without touching on either side, so that <del>a</del> the sand that you will pour in it will be of equal thickness <del>as</del> everywhere, &amp; <corr><del>is</del></corr> exceeds everywhere by the height of two good <ms><bp>fingers</bp></ms> the top of the <del>such</del> plant. And having secured the <tl>wire stem</tl> well, pour quickly <del>wet</del> your wet sand, much clearer than the one for <al>snakes</al>, in the <mu>mandore</mu>. And the sooner the better, in order that the <m>eau-de-vie</m> does not dry. And take heed to put in a little more <m>water of sal ammoniac among the common</m> than you would do for the <al>snakes</al>. And when you will make sand especially for your bouquets, where you would mix in a little more <m>feather alum</m>, it will be that much better. Thus your <tl>mold</tl> will be in one piece and it will not be necessary to unjoin it, but rather <del>leave</del> separate it from the <m>clay</m> once it will have set, let it dry, and then reheat it again until the plants are burnt. <del><fr>peys</fr></del> And note that if the plant you want to cast has a strong stalk &amp; stem, you can cast it lying down, as had been said. But if it is some weak &amp; delicate <add>flower</add>, <del>cast</del> plant it upright with the <tl><m>wax</m> peg</tl> because the sand will always <del>cast</del> lift it up, it being very clear. Do not forget to adapt two vent holes with two <tl>small sticks</tl>, starting at the foot of the cast, which is the pointed end of the <tl><m>wax</m> peg</tl>.</ab>

<ab>  
<margin>left-top</margin>  
If the plants are so delicate that they rise to the top when you pour the wet sand, one can stop and contain them with a <tl>thread</tl> passed through the circle of the <tl>mold</tl> with a <tl>needle</tl>.</ab>

<figure>

<id>fig\_p117r\_1</id>

<margin>left-top</margin>

<link><https://drive.google.com/open?id=0B9-oNrvWdlO5WnpBbm8wN2gyTWs></link>

</figure>

<figure>

<id>fig\_p117r\_2</id>

<margin>left-middle</margin>

<link><https://drive.google.com/open?id=0B9-oNrvWdlO5VURRYzlWOFByNzQ></link>

</figure>

<ab>  
<margin>left-middle</margin>  
The more delicate the fllower is, the clearer the sand must be.</ab>

<figure>

<id>fig\_p117r\_3</id>

<margin>left-bottom</margin>

<link><https://drive.google.com/open?id=0B9-oNrvWdlO5dVB5bzVUWWJuS0U></link>

<caption><tl>Mold <fr>en noyau</fr></tl>.</caption>

</figure>

</div>