<page>138v</page>

<image><http://gallica.bnf.fr/ark:/12148/btv1b10500001g/f282.item.r=></image>

<div>  
<id>p138v\_1</id>  
<head><m>Talcum</m> mixed with the molds</head>

<ab>I used the one from which I had extracted the <m>oil</m>. I crushed it very finely even more into a <m>steel</m> mortar with a pestle <x>which was</x> rough like a file. I crushed it very finely into a cottony, downy powder. I mixed it with the <m>sand</m> and soaked both matters together, and I casted it en noyau. It molded very clean and there is no doubt that it will withstand fire.</ab>

</div>  
<div>  
<id>p138v\_2</id>  
<head><m>Gold</m> casted very thinly</head>

<ab>When goldsmiths have to solder something quickly but don't have enough time to forge it, they melt <m>gold</m> and then they pour it on a cloth or on anything else that withstands fire. Then they flatten it swiftly with a hammer or another similar tool, and it <x>the gold</x> is very tenuous and it even retains the impression of the cloth.</ab>

<ab>Unalloyed pure <m>gold</m> can be cast into a medal but not into herbs and lizards or other very delicate things if it is not alloyed.</ab>

<ab>A <m>pansy</m> which is <m>oiled</m> with <m>wheat oil</m> can be cast with alloyed <m>gold</m>.</ab>

<ab>And other fruit <m>leaves</m>, but with branch<x>es</x> that are not large and especially the leaves, once cast, can be soldered.</ab>

</div>

<div>  
<id>p138v\_3</id>  
<head><m>Counterfeit diamonds put in a work</m></head>

<ab>Give a light coat on the inside of the setting with <m>black wax </m>for <fr>esbaucher</fr>, then grease the inside, thus waxed, with <m><pa>wheat</pa> oil</m>, &amp; then powder this with <m>lamp smoke</m> for it is necessary that <del><fr>ceste</fr></del> its color not have luster for <m>false stones</m>. This done, set in your <m>stone</m> <del><fr>&amp; puys</del> with a bit of <m>wax</m>, then with a <tl><m>steel</m> point</tl> &amp; a <tl>small finishing hammer</tl>, join the edge of the setting to the <m>stone</m> in order that <env>daylight</env> does not enter in. But keep from knocking the <m>stone</m>, which would break.</ab>

</div>