<page>148r</page>

<image>http://gallica.bnf.fr/ark:/12148/btv1b10500001g/f301.image</image>

<div>

<cont/>

<id>p147v\_4</id>

<ab>not come out as clear as I wanted. I reheated it again, let it cool, put it into the <m>bleach</m> again, and brushed <x>it</x>. It came out very clear. In this way, you will do <x>the same</x> for <m>copper</m> and <m>silver</m>. And if you want to give...</ab>

</div>

<div>

<id>p148r\_1</id>

<head>Beautiful color for <m>latten</m></head>

<ab>Having cleaned it well, as is said, &amp; wire-brushed it well, make it boil in water &amp; <m>turmeric root</m> or <m><fr>terra merita</fr></m>, and it will become very beautiful.</ab>

</div>

<div>

<id>p148r\_2</id>

<head><m><fr>Whitening</fr></m></head>

<ab>If it is for <m>silver</m>, do not pestle your <m>tartar</m> with <m>iron</m>, but with the handle of a hammer, for if you touch &amp; dip <m>iron</m> in your whitening, the <m>silver</m> would become red like <m>copper</m> &amp; you would need to reheat it &amp; put it again in <m>whitening</m>. Mix nothing with your <m>tartar</m> that should not enter the <m>whitening</m>, for this corrupts it. Do not let it spill out of its first boil, for in this is all its strength. The <m>whitening</m> is made with one part pulverized <m>tartar</m> &amp; a half of common <m>salt</m>.</ab>

</div>

<div>

<id>p148r\_3</id>

<head>Moulding the foot of the bittern, or of the eagle, or of other birds for the foot of saltcellars or vases</head>

<ab>One usually molds the foot &amp; the leg up to the joint. And for this effect, one molds it in five pieces: the leg in two pieces, the top of the foot in two, and the bottom in one piece.</ab>

<ab><margin>left-bottom</margin>in three pieces</ab>

</div>

<div>

<id>p148r\_4</id>

<head><m>Crocum ferri</m></head>

<ab>To make this quickly, redden the <m>filings</m> in an <m>iron</m> case, stirring it often. Then sprinkle it with good <m>vinegar</m> &amp; let it evaporate &amp; without removing it from atop the fire, <del>rou</del> let it redden &amp; inflame. Once cooled, pulverise it on the <m>marble</m> &amp; return it to the fire, sprinkle with <m>vinegar</m>, and then inflame. Thus it will quickly be colored &amp; made fine.</ab>

</div>